## Slide 1: Dirax

## Slide 2
A.J.M. Duisenberg,
J. Appl. Cryst. (1992). 25, 92-96.

## Slide 3: help
Typing “help” will open a webpage with the manual.
Typing “help commandname” will open a webpage with the manual entry for the commandname. Example: “help acl”

## Slide 4: Important
The program dirax will always give a primitive unit cell (P cell).
The program “rmatrix” can be used to find higher metric symmetry (Bravais centering)

## Slide 5: laboratory system
Z-axis: rotation axis (“omega”)
X-axis: direction from the crystal to the source
Y-axis: completing the right-handed Cartesian system

## Slide 6: rmat
The rmatrix is build by the components of the reciprocal axes in colums
x,y,z: laboratory system
Note: This corresponds to the Nonius CAD4 definition

## Slide 7: Example
RMAT P -0.15848170 -0.02721210 -0.03594000 -0.09963430 -0.02403140 0.05858360 0.06596800 0.19457920 0.00225960 TMAT P -3 1.00000000 0.00000000 0.00000000 0.00000000 1.00000000 0.00000000 0.00000000 0.00000000 1.00000000 SIGMA 0.00025 0.00134 0.00061 0.00811 0.00467 0.00416 0.05404
Note: The TMAT is applied to direct axis matrix (dmat)
Note2: The TMAT gives the possibility to save the Bravais centering and the point group.

## Slide 8: Read drx-file
With the command “read” you read the drx-file

## Slide 9: go
The command “go” starts the initial indexing.
The column Acl contains a unique identifier for every indexing solution
The column nH displays the number of indexed reflections
The program automatically selects an Acl
With the command “acl” the user can manually select an Acl

## Slide 10: indexfit
The command indexfit can be used to relax the criterion, if a reflection is considered indexed (H) instead of non-indexed (n)
Remark: preferably used if indexing was already successful.

## Slide 11: Example: indexfit 2

## Slide 12: Example: indexfit 4

## Slide 13: levelfit
Relax criterion if a reflection is considered indexed (H) instead of non-indexed (n)
Remark: preferably used, if indexing fails

## Slide 14: store
Stores indexing solution in internal memory

## Slide 15: lchi
Inverts current index status:
  indexed (H) becomes non-indexed (n)
  non-indexed (n) becomes indexed (H)

## Slide 16: compare
Compares different indexing solutions
Example: compare a b (compares solution a with solution b)

## Slide 17: savermat
The command “savermat” writes the indexing solution (rmat) into file